# Specifications of a diamond window at TPS 14A beamline

National Synchrotron Radiation Research Center

101 Hsin-Ann Rd., Hsinchu 30076, Taiwan

2026年8月11日

The National Synchrotron Radiation Research Center (hereinafter referred to as "NSRRC")

shall be pleased to receive full details of your quotation in accordance with the following terms and conditions:

# Overviews

The document is for the bid of a diamond window at TPS 14A beamline at Taiwan Photon Source in Hsinchu Taiwan.

# Scope of the contract

The vendor should provide:

- One diamond window.

- Factory test report.

# Specifications

The specifications of the diamond window are listed below(See figure 1):

- Position: at the end of the beamline.

- Function: seal off the vacuum between the beamline and the air.

- Material: CVD diamond, optical quality, single crystalline

  - flat faces polished, surface roughness <20nm RMS

  - Thickness: 300µm±50µm

  - Wedge <0.1°.

  - Side faces laser cut.

  - Diameter: 18-20mm, clear aperture: 15mm+/-0.5mm.

- The diamond window is braze-sealed into a Conflat UHV flange.

- Flange: standar 4.5 inch conflat(DIN: DN63CF).

- The window is bakeable at 200°C.

- The window should be tested to 1 bar differential pressure.

- Water cooling: water channel in CF63 flange with 6mm ϕ tubes.

- Leak rate <1×10-10 bar·cm3/s He.

# Inspection and Acceptance Criteria

## General terms

- In order to meet these specifications, NSRRC reserves the right to inspect and require alterations of the completed design.

- Agreement between NSRRC and the vendor on the entire design drawings must occur before any actual fabrication process begins.

- Unless otherwise specified in the contract or order, the vendor is responsible for the performance of all inspection requirements as specified herein.

- Except as otherwise specified, the vendor may utilize his own facilities or any commercial laboratory acceptable to NSRRC.

- A written report of the tests shall be provided to NSRRC to verify compliance with the specifications. Test methods, criteria and measuring equipment should be shown in the test report.

Factory acceptance tests

Figure 1: Conceptual drawing of the diamond window.

4.5” Conflat

Factory acceptance tests report shall provide the following test items:

- Exterior appearance check

  - Configuration should accord with the approval drawing.

  - No flaw, dent, scratch and fouling that affect the equipment in use and/or in function.

  - No sharp edges and corners.

- Dimensional check
tolerance=+/-0.1mm.

- Material certification for CVD diamond window

- Pressure Test

- Leak test

# Packing and Shipping

The finished components must be thoroughly clean and free from any organic materials or cutting fluid. The equipment must be packed in such a way that foreign materials cannot penetrate inside. The packaging methods must be subject to approval by NSRRC.

Package for shipment must ensure that the equipment is insulated from any severe shock. Markings indicating the fragile nature should be on the outside wall of the container.

The quoted item(s) shall be completed, packaged, delivered DPU NSRRC unloaded (Incoterms 2020) by the vendor.

The shipping address is:

National Synchrotron Radiation Research Center

101 Hsin-Ann Road, Hsinchu 300092, Taiwan

Attention: Dr. Chi-Yi Huang

Besides the shipping address, the following is to be displayed clearly on the outside of the packaging:

- NSRRC contract number

- Weight of the loaded package

- Support points for transport and lifting

- Tilt indicators

- Shock indicator

- Dimensions of the box

# Warranty

- The vendor warrants that all Contract Product(s) delivered by the vendor to NSRRC shall be of new manufacture, free from defects in material, workmanship.

- The warranty will remain in force for 12 months from installation and NSRRC's acceptance.